## Slide 1
Mono-
chromator
LED
Signal analysis
probe light
pump light
PIA
EASAC, KVA, Stockholm, September 19, 2013.
Hybrid Inorganic-Organic Photovoltaics, HI-OPV
Anders Hagfeldt, Uppsala University
Center for Molecular Devices
Fundamental research
Materials development
Up-scaling and process development
Dyenamo AB
www.dyenamo.se
Materials for solar cells and solar fuels research.

## Slide 2
Uppsala University
Physical Chemistry:
Anders Hagfeldt
Gerrit Boschloo
Erik Johansson
Leif Häggman
Nick Vlachopoulos
Susanna Eriksson
Marina Freitag
Lei Yang
Yan Hao
Dongqin Bi
Byung-wook Park
Hanna Ellis
Jinbao Zhang
Wenxing Yang
Meysam Pazoki
Kerttu Aitola
Valentina Leandri
Center for Molecular Devices (CMD)
Physics:
Håkan Rensmo
Rebecka Lindblad
Johan Oscarsson
Azhar Zia
Swerea IVF, Mölndal
Henrik Pettersson
Tadeusz Gruszecki
Jan Preisig
Elis Carlström
KTH Stockholm
Organic Chemistry:
Licheng Sun
Yunhua Xu
Martin Karlsson
Erik Gabrielsson
Bo Xu
Haining Tian
Inorganic Chemistry:
Lars Kloo
Gunther Andersson
Mikhail Gorlov
James Gardner
Johnny Slätt
Muthuraaman Bhagavathi Achari
Viswanathan Elumalai
Majid Safdari
Jiajia Gao

## Slide 3
Mesoscopic Dye-sensitized Solar Cells (DSC)
– a versatile and complex molecular system
The paradigm shift by O’Regan and Grätzel in 1991 meant that we can prepare efficient solar cells without using well-defined and ultrapure (expensive) semiconductors. Instead we can design molecular and nano-structures and interfaces with optimal electron transfer kinetics and rely on diffusion as charge transport mechanism -
a lot of chemistry to do!
Brian O’Regan and Michael Grätzel
Nature, 1991, 353, 7377. 7% efficiency.
> 10’000 citations

## Slide 4
DSC is a versatile (chemical) device!
Water splitting devices
Mesoscopic solid-state solar cells
Perovskite solar cells
Q-dot sensitized solar cells
-
+
Tandem Cells
n-type DSC
p-type DSC

## Slide 5
Power conversion efficiency (PCE)
laboratory cells: 13.0 % (EPFL), modules: 9.9 % (Sony).
Perovskite solar cells. 14.1% (certified, EPFL), about 15% (EPFL, Oxford)
Outdoor performance - production cost per kWh an advantage for DSC:
a 10 % PCE rated DSSC module produces over one year the same amount of electricity as 14-15 % rated Si module (Sony).
Electricity from ambient and indoor light:
DSC outperforms all competitors
stability
> 20 years outdoors accelerated testing (Dyesol, Fujikura …)
energy pay back time:
< 1 year (3GSolar and ECN life cycle analysis
Some DSC facts

## Slide 6
6
HANA AKARI
FLOWER LAMP
(SONY)
Design: Colours and Transparency
Product Integration
Notes: 6

## Slide 7
Façade for the new congress hall at EPFL, Lausanne
Building Integration

## Slide 8
How to compete with silicon?
  Production cost of 50 $/m2 with 15 % module efficiency gives 0.33 $/Wpeak
  Cell efficiencies > 15%?
  - Two recent breakthroughs from the DSC community
  - The hunt for the half volt –replacing the I-/I3- redox couple
  - Perovskite solar cells

## Slide 9
TiO2
e-
e-
e-
Dye
TCO
Electrolyte
e-
e-
e-
Dye-sensitized Solar Cells
Where are the internal losses?
- the hunt for the half volt
I- / I3-
Can a 2-electron redox couple be replaced by a 1-electron couple?
A problem for almost 20 years

## Slide 10: In 2010 we introduced the ’marriage’ between a blocking dye and Co-complex redox systems
D35
Feldt, Gibson, Gabrielsson, Sun, Boschloo, Hagfeldt,
J. Am. Chem. Soc. 2010, 132, 16714.

## Slide 11: Best result with Co-mediator without steric groups: - Electron lifetimes the same for all Co-mediators - Mass transport best for Co-mediator without steric groups - Suitable for indoor light
 | Voc / V | Jsc / mAcm-2 | FF | η / %
[Co(bpy)3]n+ 1 sun 1/10 sun 250 lux | 0.92 0.85 0.7 | 10.7 1.12 18.5 x 10-3 | 0.68 0.76 0.8 | 6.71 7.15
0.22 M Co-red, 0.033 M Co-ox, 0.1 M LiClO4 and 0.2 M 4-tert butylpyridine (TBP) in acetonitrile

## Slide 12: The World Record DSC is Based on Porphyrine Dye and Co-complex Redox Electrolyte
Grätzel and co-workers: The SM315 porphyrin
reaches a record efficiency of 13% :

## Slide 13: Solid-State DSC
Solid hole conductor PCE
Redox electrolyte PCE
dye
DSSC using hole transport material
DSSC using redox electrolyte
TiO2
TiO2
light harvester
dye or pigment film

## Slide 14
Solid-state DSSC
In collaboration with BASF SE and EPFL.
ID176 + spiro-OMeTAD
Works well for ssDSSC (> 3%), but very poor in liq-DSSC (<1%)
Cappel et al. J. Phys. Chem. C, 2009, 113, 14595
spiro-OMeTAD
ID176

## Slide 15: Why does ID176 work in solid and not in liquid DSC?
Spiro-OMeTAD
ps regeneration
CB
Cappel et al. JPC C, 2011, 115, 4345
1
2
Reduced Dye
Excited state
3
B.
Injection in surface states?
A.
Ultrafast regeneration of the oxidized dye.
Reductive quenching mechanism.

## Slide 16
-
-
-
-
+
Reductive quenching may allow for electron
conduction through a dye/ETA layer
*ETA = Extremely Thin Absorber
Ultrafast regeneration by
solid-state hole conductor
Dye/ETA layer

## Slide 18: Perovskite Solar Cells - An Organic-Inorganic Hybrid

## Slide 19
Cross sectional SEM of a mesoscopic p-i-n solar cell with
TiO2/perovskite as light harvester
P
i
nanocomposite
n
Certified record efficiency of 14.1% by Grätzel and coworkers.

## Slide 20
Best efficiency, 10.8%, obtained with ZrO2 as scaffold.
Our latest perovskite results from CMD
RSC Adv., 2013, DOI: 10.1039/C3RA43228A

## Slide 21: Several open fundamental questions
Perovskites work on insulating substrates like ZrO2 and Al2O3. Is electron injection necessary?
Works without the p-type hole conductor (direct contact between Au and perovskite).
Low exciton binding energy (30 – 50 mV). Selective contact device?
Reproducibility (morphology of perovskite vs preparation conditions)
Stability: for a single crystal perovskite there is e.g. A phase transtion at 55 0C (from tetragonal to cubic)
Possibilities to replace Pb?
Opens up 3rd Generation concepts?

## Slide 22
The possibilities for efficiencies >15%
Absorber with band gap of 1.6 eV (ca. 800 nm)
0.25V for driving force for injection and regeneration
Possible efficiency:
Voc=1.1V, Jsc= 22 mA/cm2, FF = 0.73.
PCE= 17.66 %
Module efficiencies of 15% possible
1.6 eV
0.25 eV
0.25 eV
V vs NHE
1.0
0.75
- 0.35
- 0.6
Cf. Grätzel et al. Nature Comm.
3 (2012) Art. Nr. 631
Cf. O’Regan et al. Chem. Mater.
23 (2011) 3381

## Slide 23
Financial Support - CMD
Knut & Alice Wallenberg Foundation
Sony Deutschland GmbH
Merck, Germany