## Slide 1: Nanowires with promise for high efficiency photovoltaics
M.T. Borgström,
magnus.borgstrom@ftf.lth.se
NW Doping
Total control over axial and radial NW growth
NW solar cells

## Slide 2: World record efficiency solar cell
Solar Junction: III-V multi junction solar cell
US energy information
administration 2012

## Slide 3: AMON-RA (FP7 214814)
Lund University
Fraunhofer Institute for Solar Energy Systems
University of Kassel
Sol Voltaics AB
Johannes Kepler University Linz
Technical University of Denmark

## Slide 4
Impurity doping in nanowires
Particle assisted growth:
Low temperature (400-500ºC) MOVPE 600-700ºC
Complex growth dynamics
[111] growth direction
crystal structure
Solubility
Segregation coefficient
Characterisation:
Chemically (EDX)
Electrically (Field effect)
Optically (PL)
Atom probe
Hall measurements
Wallentin, Borgström JMR 2011

## Slide 5: Evaluate doping – nw-FET
Drude model,  nq
Carrier concentration, n = doping concentration
Mobility (µ) extracted from gate-sweeps
Conductivity (σ) extracted from I-V
n-type

## Slide 6
TESn for n-doping
(Sn:InP ionization energy 5.9 meV)
Gate voltage dependent action - n-type
transconductance + IV (ohmic contacts)
threshold voltage (non ohmic contacts)
Borgström et al, Nanotechnology, 2008

## Slide 7: Dimethylzinc for p-doping (Zn:InP ionization energy 35 meV)
Gate voltage dependent action - p-type
DMZn enhances the nanowire growth rate and suppresses side wall growth
Nucleation problems for high dopant precursor molar fraction
XDMZn=1e-6, 20min
XDMZn=1e-5, 20min
XDMZn=5e-5, 20min
Borgström et al, IEEE J Sel Top Quant 2011

## Slide 8: Decoupled axial and radial growth
Increasing in-situ HCl molar fraction
80 nm aerosol particles
TMI, PH3, HCl
Growth temperature 450C
Borgström et al, Nano Research, 2010

## Slide 9: NW solar cell fabrication
1x1 mm devices
Borgström et al, IEEE J Sel Top Quant 2011
ITO
InP:p+
InP:p
InP:n
Di-
electric

## Slide 10: Photocurrent measurements
Efficiency 3.8% (1 sun, AM 1.5)
Fill factor 74%
Voc = 0.75 V
Excellent light capture despite
low density (are fill factor 3%)
5 times more efficient per active
surface area than thin film InP cell
Current density through NW
about 3 times higher than in record
multi junction solar cells.

## Slide 11: Modeling ideal structures
t=2000 nm
Anttu & Xu,
Optics Express, 2013

## Slide 12: Nano imprint lithography for large scale economically viable patterning

## Slide 13: Nano imprint lithography for large scale economically viable patterning

## Slide 14: PV performance
NW surface fraction 12%
Wallentin et al, Science 2013

## Slide 15: Summary
NWs promising for high efficiency solar energy harvesting
NW Doping
Nano imprint lithography for NW growth
Nanowire based photovoltaics

## Slide 16: Acknowledgements
EU project AMON-RA (FP7 214814)
EON International Research Initiative.
Swedish energy agency
Swedish Research Council
Swedish Foundation for Strategic Research
J. Wallentin, N. Anttu, D. Jacobsson, M. Heurlin, H. Q. Xu, L. Samuelson, K. Deppert
Solid state physics, Lund University
D. Asoli, M. Huffman, I. Åberg, M. Magnusson
Solvoltaics AB, Lund
M. Ek, L. R. Wallenberg
Polymer & Materials Chemistry/nCHREM, Lund University
J . Persson, J. Wagner
Center for Electron Nanoscopy, Technical University of Denmark
D. Kriegner, T. Etzelstorfer, J. Stangl, G. Bauer
Johannes Kepler University Linz
P. Kailuweit, G. Siefer, F. Dimroth
Fraunhofer institute for solar energy systems, Freiburg