## Slide 1: Lactid Acid, Ionic Liquids and Energy Materials: Perspectives of Hydrothermal Biomass Upgrade
Markus Antonietti, Nina Fechler, Tim Fellinger
Max Planck Institute of Colloids and Interfaces
Research Campus Golm, D-14424 Potsdam
Stockholm, Renewables 2013

## Slide 2
Addressing the “CO2@chemicals-problem”
a chemists balance on the back of an envelope
annual world oil production 4 km3
oil generates about 15 GT CO2 per year
GLOBAL CARBON MINUS: ca 10 Gt
annual world terrestrial biomass growth 120 km3
6,7 % of biomass sufficient to compensate for fossile
CO2 generation
11 % of biomass already part of farming cycles
    “personal” foodstep: 3.0 tons
    We need CO2- negative technologies & products

## Slide 3: A problem and a chance: the misrelation of product and „waste“

## Slide 4: Towards a „covergent“ technology: the biorefinery approach
refinery
biorefinery

## Slide 5
The use of complete biomass in biorefining
„top cut“ 0.1 % (e.g.patchoulol)
„medium cut“
30 % platform chemicals
e.g. lactic acid, green solvents
„base cut“
70 % „fertility, fuels and energy“
e.g. methane, coal, fertilizer and humic matter

## Slide 6
Aqueous HTR-processes
provide new platform chemicals
Lactid Acid
Gamma-butyrolacton
HTR = hydrothermal reforming/digestion

## Slide 11
Same intermediate scheme: „Bio –ILs“
approach here:
„fundamentalistic“ green chemistry:
In water, near room temperature, no catalysts, equimolar reactands
Debus-Radziszewski- reaction
1858
sugar + amino acid /amine

## Slide 12
The Laevulic acid story
γ -methylbutyrolacton (γ-MBL) is a diesel replacement, LD50 higher than ethanol…

## Slide 13
Hydrothermal Reforming/Conditions
20 min
data
fundamentalistic green

## Slide 14
Real chemistry: H2 and Ni/Bio-Ni-Catalyst
Current work with MPI Mülheim:
Cellulose  Glucose
H2SO4  Laevulic Acid
LA  MBL
Estimated overall yield 60% (straw)
Side product: lignin, „humic acids..“

## Slide 15
The use of complete biomass in biorefining
„top cut“-10 % (e.g.food + fibers)
„medium cut“
30 % platform chemicals
e.g. lactic acid, green solvents
„base cut“
70 % „fertility, fuels and energy“
e.g. methane, coal, fertilizer and humic matter

## Slide 16: After HTR: Hydrothermal Carbonization
a technique to turn plant material
into monomers
into polymers
into carbonaceous materials
all in water
 colloid and interface chemistry
Carbon efficiency ≈ 1
Friedrich Bergius described 1913 the elemental steps of HTC

## Slide 17: Hydrothermal Carbonization
works via dehydration of carbohydrates
at 180 °C – 200 °C
for 2 – 16 h´s
C6H12O6 __ C6H6O3 + 3 H2O  C6H2O + 5 H2O
quite cheap ( ca. 0.40 €/kg starch, 100 €/t biomass)
leads to useful nanostructures
with useful interface chemistry
„the dispersion polymerization of carbon“

## Slide 18: Carbonaceous structures to be made: (all from glucose/starch/biomass)

## Slide 19
„designer-carbons“
noble carbon (N-C)
Carbons new
to
mankind

## Slide 20
Case for Discussion:
Designer-Carbons for Energy Storage
the „race“:
Batteries versus Supercapacitors
I believe: Supercapacitors !
(but why ?)

## Slide 21: Supercapacitors made of N-containing Biomass
Potential to beat all current storage technologies (availability, price)
10 kg Material: 160 KW for 12.5 Sec.
Notes: 21

## Slide 23: Energy Storage: Some lecturing
Supercapacitor: 300 F/g @ 1 V  1 e- for 320 mass units
Capacitance of graphene/nanotubes: metallic theory
100 F/g,  1 e for 80 C-atoms
(Phys. Rev. E 83, 056102 (2011)
Pseudocapacitance
≈ 1.600 F/g
( polyaniline 1.100 F/g
Ni-foam 2018 F/g )
Energy density = 150 VAs/g = 42 mAh/g @ 1 V ( beats Pb-technology!)
Potential: E= ½ CU2 - higher U: ionic liquids!
- higher C: carbon chemistry

## Slide 24: Own work on superporous carbons for Redox- Supercapacitors
Salt templating with Q/HQ (2013)
with PANI (2007)
visible: 1kWh/kg, price 5-10 €/kg ??

## Slide 25
The Birch reduction as a charge
storage mechanism
(again:)

## Slide 26: The Leitbild: decentral private energy storage as a key tool of the intelligent grid
Every private home has a –say- 1t electricity storage in the cellar (every windmill 10 t)
You buy electricity only when it is cheap and available (buffer)
Current fiction based on (top) science predicts 4 GJ/ton
ca 1 kWh/kg = 1000 kWh buffer capacity
economy: saves 1000 Euro/year per family
Secondaries: savety, price (maybe 5 -10 Euro/kg)

## Slide 27: Noble carbon  flame retardance

## Slide 28: A pilot plant, VC & MaxPlanckSociety

## Slide 30
N-doped carbon (highly conductive, catalytically active, etc.)
Precursor: imidazolium- and pyridinium-ionic liuqids.
Electrospinning: powerful tool to prepare fibers and mats / membranes.
Project: prepare N-doped carbon membranes by electrospinning
PIL for N-doped carbon membranes
Polym. Chem. 2011, 2, 1654

## Slide 31
Carbon mats / membranes
N content : 6.33%
At 1000°C

## Slide 32
Carbon membranes
N content : 8.00%
Conductivity: 200 S/cm

## Slide 33: Dynamic Performance as an electrode
C/N-Monolith
Comm. fuel cell carbon fleece
Notes: 33

## Slide 34: ORR: “Metal Free” O2-Activation by Porous N-doped carbon materials
all data: Dr. Wen Yang, Tim Fellinger, Nina Fechler
JACS 2011
Highly conductive, highly noble, basic:
an electrocatalyst !
Hybridisation with nucleobases
dissolve in ILs
Increase of N-content to 15 wt%
Notes: 34
34

## Slide 35: Electrochemistry- ORR
Rotating-disk voltammograms recorded for Meso-Em/nuclebase and 20 wt % Pt-C in O2-saturated 0.1 M KOH.
Notes: 35
35

## Slide 36: Electrochemistry-Stability
Notes: 36
36

## Slide 37
The newest generation:spin bopper
acidic !
alkaline
stability test
0.05M H2SO4,
O2, 1600rpm

## Slide 38: C/N on Nickel foam: Oxygen liberation
0,1M KOH
Pt as counter electrode
Ag/AgCl as reference electrode

## Slide 39
The other side: C/N@FTO: H2-liberation

## Slide 40: Electrochemical Synthesis of H2O2
Price: 2.4 cents kg-1 H2O2
at 10 cents per kWh-1 !
With Tim Fellinger, Peter Strasser, Frédéric Hasché

## Slide 41
graphitic C3N4
an organic semiconductor, from sustainable usea
Liebig, 1834
Jürgens et al., JACS 2003
Liu et al., Science 1989
A big jump: 5 slides on carbon nitride

## Slide 42
Band positions: ideal for the photocatalytic water splitting

## Slide 43: H2 evolution on Pt (0.5 wt%)-loaded C3N4
l > 420 nm
Catalyst, 0.1 g, Reactant solution, aqueous triethanolamine solution 100 mL 10 vol.%; Reaction vessel, Pyrex top irradiation-type; Light source, xenon lamp (300 W) attached with a cutoff filter
H2
N2

## Slide 44: Photochemical Cofactor regeneration (a Frankensteinian experiment)
the NAD+/NADH couple
Sub
H-Sub
Enzyme

## Slide 45
NADH-generation under optimized conditions: Coining Light energy into biological currency

## Slide 46
Conclusion
  biorefining: HTR and HTC
  Lactid acid, IL-monomers, Γ-MBL
  supercapacitor carbons: performance@batteries
  noble carbons: spinneable electrodes
  new designer carbons
  ORR catalysts, O2 and H2O2 generation, metal-free
  optical NADH-regeneration, now electrochemical ??
  closing the missing pieces in biorefinery schemes

## Slide 47
Chemistry with a
golden-green
future

## Slide 48
the Carbon-
people
Thanks to those who really did the work:
Notes: 48

## Slide 49
Department of Colloid Chemistry
MPI of Colloids and Interfaces
Thanks to the Max Planck Society:
Research for long term problems
ENERCHEM 2005 ERC2008