## Slide 1
Michel Armand
“Electrochemical energy storage, activity on all fronts”
Charred Boeing 787 Dreamliner Battery
CNRS – Université de Picardie Jules Verne – France
CIC Energigune, Vitoria – Spain
Deakin University, Melboure – Australia
EASAC Stockholm Sep 19 – 20 2013
Notes: PORTADA

## Slide 2
Our forefathers…
- . Furthermore, sodium batteries are the most energetic, and their electromotive force is double that of zinc cells.
Jules Verne Twenty Thousand Leagues Under The Sea Hetzel Publisher, Paris 1870
- Sodium?
- Yes Sir. Mixed with mercury, it forms an amalgam which replaces zinc in Bunsen cells. The mercury lasts forever. Only sodium is consumed and the ocean provides it.

## Slide 3
1 Billion Cars in 2010 and ➚
…and 1.3 106 fatalities on the roads!
> 2 106 premature deaths from air-borne particles in big cities

## Slide 4
Needs for electrochemical storage…
Automobiles
Load-levelling
1.109 cars 10% electric
 20.106 tons batteries
World electricity production
= 2.1013 kWh 10% stored/day
 60.106 tons batteries!
Sustainability a prime criterion!
Notes: EJEMPLO PANTALLA

## Slide 5: The periodic table according to abundance

## Slide 6: Elements and mankind
20 tons of CO2 / ton of Al
2 ton of CO2 / ton of Fe
50 tons of CO2 / ton of Cu!
CO2 signature of copper to increase further!

## Slide 7: Energy and transportation…
• Charger/transformer 90%
• Battery C/D efficiency 90%
• Power electronics 98%
• Electric motor 91%
Without regenerative breaking

## Slide 8: The“100” rules
 Batteries capacity @ 100 Wh /Kg = 1% of hydrocarbons energy content
 Evs: 100 Km of driving range per 100Kg of battery weight
 EV consumption @ 100 Wh/Km/ton
 100 W/Kg = Charge/discharge in 1 hour “C” rate

## Slide 9
Li° Solid-state batteries
T > 50°C
Polymer
liquid
liquid
gel
Li-ion batteries
-20 < T < 55°C
Future gel, ionic liquid or all solid
higher capacity?
Li batteries of all sorts…
Copper

## Slide 10
Temperature of operation
3 Families of electrolytes
Glasses: SiS2/Li2S/LiI
Tg ≈ 270°C; tLi+ = 1
Liquids: LiPF6 in EC
Tg ≈ -100°C; tLi+ = 0.3
PEO / [(LiCF3SO2)2N]
Tg ≈ -40°C; tLi+ = 0.3
300 m2 of electrolyte, electrode for an EV battery

## Slide 11: Aging / Failure modes
Li-ion
LMP

## Slide 12: Driving Range
Li-ion = 150 km
Lithium metal / polymer = 250 km
Taxi on average ∀ country ≈ 230 Km/day
http://www.autolib.eu/
Nissan Leaf
• 60 kg of Co° (or Co + Ni/Mn)
• 40 kg of Cu°
• 7 kg of Li°
• 70 kg of Fe°
• 10 kg of Cu°
• 10 kg of Li°

## Slide 13: A Solid-State System in Not a View of the Mind
Autolib®:
2000 cars on a ”pay and ride”
basis
250 Km driving range
C/4 charge rate

## Slide 14
Liquid Electrolytes
Polymer Electrolytes
T
climate
-40°C
+50°C
Under the hood
+80°C
RUNAWAY !!
Operation starting
> 220° Runaway!
- 20 °C Electrolyte freezing
Electrolyte boiling
180° Lithium melting

## Slide 15
Liquid Electrolytes
T
climate
-40°C
+50°C
Under the hood
+80°C
RUNAWAY !!
- 20 °C Electrolyte freezing
Electrolyte boiling
Polymer Electrolytes
Operation starting
> 220° Runaway!
180° Lithium melting
!
Lithium metal plating

## Slide 16: National transport Safety Board

## Slide 17: Safety again with solid electrolytes…
5 autolib cars were torched in the Paris suburbs…
Courtesy Bolloré

## Slide 18: Towards 2 electrons / Transition Metal…
Potential vs. composition for the system
Li2-xFeSiO4-yNy for y = 0.5 and y = 1
De Arroyo et al. J. Mat. Chem., 21(27), 10026 (2011).

## Slide 19
t+ = 1 polymer electrolytes …

## Slide 20: 4 electrochemical contenders
Copper current collector
Al current collector
Very little metal used

## Slide 21: Conclusions…
• Li° polymer batteries DO exist with GREEN LiFePO4 no Cu° and up to now meet SAFETY tests; a 60°C operation is a plausible and desirable goal. Probably not for grid.
• Mg is a decisive advantage only if its double charge induces 2 electron reaction: MgMnIISiO4  MnIVSiO4 (cf LiFeIIPO4  FeIIIPO4). But in limbos!
• Focus on sodium-ion for smart grid storage. High temperature Na/S > 50 MWh installed
• Batteries directly extrapolated from micro-electronics to Evs (even more grid!) are probably a dead-end due to unsustainability, short life-time and safety
• Make all this electrochemistry as slurry to use in redox-flow cells. Decoupling capacity from size of the cell. Replacement of VV + VIV / VIII + VII (20 Wh/kg)!

## Slide 22: Renault and Bolloré in electric car deal
http://www.ft.com/intl/cms/s/0/49ca1de2-1bc8-11e3-94a3-00144feab7de.html
Sep 12, 2013

## Slide 23: Thank you for your attention

## Slide 24: A “Down to Earth” Approach to Energy Density
Realistic charge
2 mAh/cm2
=
“Sand Charge” f(σ, t+ D)
specific capacities
Composite:
Volume fractions
Composite?
Volume fractions

## Slide 25
Why lithium?
Li+ is able to diffuse in most solid structures or cleave many metallic or ionocovalent bonds
 metallic Lithium
Lithium intercalated in graphite 
Oxides (lamellar)
LixCoO2, LixV2O5 but 3D (LiMn2O4)
Strong oxidizing agent
positiveelectrode
Strong reducing agent
negative electrode 

## Slide 26: Classical LMNO li-ion …
LiC6+ 1.25Li0.2Mn2O4 C6 + 1.25LiMn2O4
Si cathode @ 175 Wh /kg

## Slide 27: Lithium-rich cathodes System …
Li4Ti5O12 +“Li-rich” Li7Ti5O12 + ☐“Li-rich”

## Slide 28: Lithium Metal System …
3Li + ☐FePO4 2Li + ☐LiFePO4

## Slide 29: Consequences of ambipolar Transport
Li+
X-
Li+
Li+
X-
Li+
depletion
conductivity  0
overconcentration
conductivity 
Dendrites Formation
Newman’s model: t+ = 1 are equivalent to
10 times more conductive t+ ≈ 0.3 electrolytes

## Slide 30
Composition-voltage behaviour of carboxylates
S. Grugeon, M. Armand, S. Laruelle, H. Vezin, P. Poizot and J.M. Tarascon (2008 Submitted
280mAh/g
35 000 T/yr available from PET recycling !

## Slide 31
t+ = 1 random polymer electrolytes …
Free anion state of the art

## Slide 32: T+ = 1 electrolytes
Nothing else but Li+ moves. Ultimate solution to no SEI, no concentration gradient. But still needs @ 60°C operation
Newman’s modeling:
1/10th of the conductivity needed for the same power output than T+ = 0.3

## Slide 33: Classical LMNO li-ion …
LiC6+ 1.25Li0.2Mn2O4 C6 + 1.25LiMn2O4
NEA: 33 % of
total weight
$ 5/m2
Si still ≈ 25%

## Slide 34: Fabrication process

## Slide 35: Sodium System…
+ NaFePO4
+ ☐FePO4
Liang Zhao , Junmei Zhao , Yong-Sheng Hu Hong Li , Zhibin Zhou , Michel Armand ,
and Liquan Chen Adv. Energy Mater. 2012,

## Slide 36: Lithium Metal System …
3Li + ☐FePO4 2Li + LiFePO4
7 % of
total weight
$ 1/m2
Li° = $ 70/kg

## Slide 37: Safety!!
Shenzen, May 27 / 2012; 3 fatalities

## Slide 38
Li
Properties
Inexpensive material

Environmentally friendly


Thermal stability of LiFePO4 and
FePO4 phases up to 400 ºC
Triphylite
Olivine structure
J. Goodenough and K. Padhi, 1996
FePO4
Heterosite
The “natural” intercalation compound a few billons years old!

## Slide 39: Electrode materials
Very poor e- 
1D ionic (poor)
Non-conductors
Radical species
2008
Discrete molecules
LiFePO4
1995
1984
Disulfides S—S
Non-conductors
First biomimetic
reactions
1972-5
Intercalation
materials
2D semi-metal
TiS2, graphite
3D Li+, e-, semi-conductor
1982
LiMn2O4
Diminishing influence of  electronic, dimensionality

## Slide 40: A chemical nightmarish cascade!
G. Gachot, S. Grugeon, M. Armand, S. Pilard, P. Guenot ,
J-M. Tarascon, S Laruelle. J. Power Sources 178-1, 409-421, (2008)
X, Y, R1-3 = H, Li, C(=O)OCH3…
Oversimplification!
Aurbach et al.
Ogumi et al.
PF5 + LiF
+ H2O  HF
!
Urgent need to replace LiPF6

## Slide 41: Nano-painting
Carbon coating ≈ 1nm thick, transparent to ions
Structured carbon black nano particles
Electrolyte